## Slide 1: Modeling of Attempt-to-Escape Frequency: Tunneling Emission of Trapped Electrons in Tunneling Oxides of 3-D NAND Flash Memory
Myung Jin and Hyuncheol Shin
10.1109/TED.2025.3589340
Font : Arial

## Slide 2: Fig. 1
Si - Channel (Ch)
Wordline (WL)
N
WL
Ch
(c)
...
nt
(b)
tCTN
(d)
Q
ΔQ0
ΔQ1
ΔQN
=
+
+
+
...
=
+
+
+
...
r0
r1
rN
...
CTN charge
ΔQi = πri2(nt,i+1-nt,i)
nt,0 = 0
nt,N+1 = 0
where, i=1-N
(a)
Cylindrical
filler
Ch
O/N/O
tTOX
tBOX
ΔQ0
ΔQ1
ΔQ2
ΔQ3
ΔQN-1
ΔQN
WL
WL
WL

## Slide 3: Fig. 2
Trap Profile [8] |  | 
Et, shallow | 0.84 | [eV]
σt, shallow | 0.2 | [eV]
Et, deep | 1.8 | [eV]
σt, deep | - | [eV]
(b)
(c)
(a)
(e)
(b)
(c)
TCAD parameter deck |  | 
μCTN | 0.1 [7] | [cm2/V·s]
σn | 1e-16 [7] | [cm2]
εO/N/O | 3.9/7.5/3.9ε0 [8] | [F/cm]
tO/N/O | 3/6/8 | [nm]
ΔVt | 1.8 | [V]
3.1 eV
1.0 eV
3.65 eV
nt
tCTN
Radial charge distribution modeled as [5], [6]

## Slide 4: Fig. 3
μ [eV] | σ [eV] | Nt [cm-3]
0.84 | 0.2 | 1.15 × 1019
1.8 | 0.05 | 3.5 × 1019
(a)
 | TCAD Simulation | Autonomous Model
Computation dependency over time domain | Every time step needed | Independent of time domain (only initial condition needed)
Simulation time | > 10000 s | < 10 s
(a)
(b)
tTOX
= 3, 3.5, 4, 4.5, 5 [nm]