## Slide 1: Time-Step-Free Physics-Based Modeling of Retention Loss in Cryogenic 3-D NAND Flash
Myung Jin, Haechan Choi, and Hyuncheol Shin
EDL-2026-06-1412.R1
(Accepted Manuscript)

## Slide 2: Fig. 1
Si - Channel (Ch)
Wordline (WL)
N
WL
Ch
(c)
...
nt
(b)
tCTN
(d)
Q
ΔQ0
ΔQ1
ΔQN
=
+
+
+
...
=
+
+
+
...
r0
r1
rN
...
CTN charge
ΔQi = πri2(nt,i+1-nt,i)
nt,0 = 0
nt,N+1 = 0
where, i=1-N
(a)
Cylindrical
filler
Ch
O/N/O
tTOX
tBOX
ΔQ0
ΔQ1
ΔQ2
ΔQ3
ΔQN-1
ΔQN
WL
WL
WL
extracted from TCAD after program

## Slide 3: Fig. 2
Trap profile [6], [9] |  | 
Et, shallow | 0.84 | [eV]
σt, shallow | 0.2 | [eV]
Et, deep | 1.8 | [eV]
σt, deep | - | [eV]
(a)
(b)
(c)
TCAD parameter deck |  | 
μCTN | 0.1 [8] | [cm2/V·s]
σn | 1e-16 [8] | [cm2]
εO/N/O | 3.9/7.5/3.9ε0 [9] | [F/cm]
tO/N/O | 3/6/8 | [nm]
3.1 eV
1.0 eV
3.65 eV
nt
tCTN
TCAD-aligned model consistent with [6], [7]
Trap density [6], [9] |  | 
nt, shallow | 1.15e19 | [cm-3]
nt, deep | 3.5e19 | [cm-3]

## Slide 4: Fig. 3
(a)
(b)
tTOX
= 3, 3.5, 4, 4.5, 5 [nm]
(c)